## Slide 1: AB INITIO (first principles) calculations short introduction
Petr Šesták
Nanomechanics lecture
sestak@fme.vutbr.cz
Brno University of Technology

## Slide 2: Multiscale modeling
length
discipline
quantum mechanics
atomistic model
microstructure
continuum model
ab initio
molecular dynamics
finite elements
nm
m
mm
m
physics – chemistry – mat. science – engineering

## Slide 3: Sample of multiscale modeling Cuticle of Homarus americanus

## Slide 4: From milimeters to nanometers
D. Raabe et al. / Acta Materialia 53 (2005) 4281 - 4292

## Slide 5: Multi-scale changes in the elastic anisotropy
Advanced Materials 22 (2010) 519.

## Slide 6: Ab initio simulations and molecular dynamics
Molecular Dynamics | Ab initio
easy – based on Newton mechanics | results from Quantum Mechanics
simulations of large scale system with planar defects, temperature | magnetic, optical, electrical, etc. characteristics
potentials require calibration (Ni-Ni, Ni-Ti, etc.) | accuracy, no input data needed
finite temperatures | no temperature – simul. at absolute zero temp.
milions of atoms | limited to small systems (approx. 100-1000 atoms)
 | standard DFT no vdW but has been impl.
requires HPC (High Performance Computing) | requires HPC (High Performance Computing)
Ab initio is very often used for calibration of MD potentials.
-
-
-
-

## Slide 7: Results replicability over ab initio codes

## Slide 8: Carbon predictions over available MD potentials

## Slide 9
Comments from scientific audience
I believe in DFT calculations but I do not believe in DFT models.
We need quantum computers!
MD potentials can reflects behavior they were tested for.
Precision must be improved!

## Slide 10
How to get DFT precision into MD??

## Slide 11: Ab initio methods (first principles)
The most used ab initio codes
based on:
DFT – Density Functional Theory*
*W. Kohn and J. L. Sham; Phys. Rev. 140 (1965) A1133
*P. Hohenberg and W. Kohn; Phys. Rev. 136 (1964) B864-871
Schrödinger | DFT – Kohn Sham equation
many body electron interaction | electron interacting with external potential created by ions and electrons
difficult to solve for more than 2 electrons | can be solved
interaction: electron-electron, ion-electron and ion-ion | 


## Slide 12: DFT self-consistent cycle

## Slide 13: Ab initio methods (first principles)
computational codes
  VASP (Vienna Ab initio Simulation Package) – pseudopotentials (www.vasp.at)
    commercial license
    it is used very often
    available pseudopotentials are very well tested
    hybrid pseudopotentials
  Abinit – pseudopotentials (www.abinit.org)
    free under GNU license
    generation of pseudopotentials by users
    some extra features than other codes (Linear Response Functions - direct calculation of phonon spectra, elastic constants, etc.)
    very good parallelization (using multithread program run)
  Wien2k – all electron (no pseudopot.) (www.wien2k.at)
    commercial license
    computationally more demanding than VASP or Abinit
    good parallelization
    no pseudopotential – all electron code
pseudopotentials
  PAW (Projector Augmented Waves), ultra-soft, norm-conserving
  exchange – correlation energy:
    LDA – Local Density Approximation
    GGA BPE – Berdew Burke Ernzerhof
    GGA PW – Perdew Wang

## Slide 14: Available codes

## Slide 15: Available codes
AND MANY MORE

## Slide 16: Pseudopotential approach
Pseudopotential is a very efficient way how to reliably describe valence electrons. Core electrons are kept frozen in their configurations – they are considered as a rigid non-polarizable ion cores while valence electrons are precisely described.
Types:
  norm-conserving – very old, inappropriate for magnetic mat.,
  ultrasoft,
  PAW – Projector Augmented Waves
  (the most used pseudopotential,
  recommended for VASP* or Abinit**).
*G. Kresse and D. Joubert; Phys. Rev. B 59 (1999) 1758-1775
**M. Torrent et al.; Comp. Mater. Sci. 42 (2008) 337-351

## Slide 17: available outputs from Ab initio simulation
the total energy of studied system (important are changes of the energy for different structure configurations)
the stress tensor along with all forces acting on each atom
phonon spectra computed by direct method or Linear Response Function
optical properties of materials
electrical properties of materials (dielectric constants)
Density of States (DOS) - band gap energy of semiconductors
charge density
structure optimization – positions and cell shape (find the structure configuration with the lowest total energy)
structure optimization under specified conditions – cell shape optimizations with constant volume, etc.

## Slide 18: Periodic boundary conditions

## Slide 19: Periodic boundary conditions Large structures

## Slide 20: Periodic boundary conditions Large structures
https://www.youtube.com/watch?v=5qdNafdyaG0
some youtube sample

## Slide 21: VASP – output examples
tensile test of graphene sheets

## Slide 22: VASP – output examples charge density
Sample of 3D charge density of 5 (210) grain boundary.

## Slide 23: VASP – output examples charge density
Sample of 2D charge density of 5 (210) grain boundary.
an impurity atom

## Slide 24: VASP – output examples: charge density
Sample of 3D charge density of graphene sheet.

## Slide 25: VASP – output examples: charge density
Sample of 2D charge density of graphene sheet.

## Slide 26: Charge density strong and weak bonds
*P. Sestak,J. Wu,J. He,J. Pokluda and Z. Zhang; Phys. Chem. Chem. Phys. 17 (2015) 18684 DOI: 10.1039/c5cp02043c59

## Slide 27: Charge density of molecules

## Slide 28: VASP – output examples: density of states
Sample of Si density of states - SEMICONDUCTOR.

## Slide 29: VASP – output examples: density of states
Sample of C density of states - INSULATOR.

## Slide 30: MD fundamental scheme
structure – initial position and velocities
topology – molecular description
force fields – potential functions V of interactions
compute forces
solve Newton equation of motion
output – position, velocities energies
update r and v in repeating in N steps
forces are determined from the DFT calculations

## Slide 31: Ai initio molecular dynamics calculations
Taking advantages and disadvantages of ab initio and MD simulations.
  disadvantages:
    the simulation space/cell is small (up to 1000 of atoms)
    only thousands of the time steps (for time step 1fs → entire time 1-10 ns)
    for the VASP the simulations are performed under constant volume
    minimal number of atoms should be at least 200 to achieve enough interaction for the MD
  advantages:
    NO potentials required
    temperature included
    precise simulations → computed from electronic density
    magnetism included

## Slide 32: First principles molecular dynamics calculations GB+H

## Slide 33: Hydrate – something went wrong

## Slide 34: VASP
www.vasp.at
  documentation
  tutorials
  forum

## Slide 35: When we should use the DFT?
Can be our problem described using a small unit cell (nanoscale, around 10nm)?
Does temperature play important role?
How many elements from the periodic table are introduced?
What quantity (physical, chemical, etc. ) am I looking for?
Validating of MD potentials.

## Slide 36: Car-Parrinello Methods www.cpmd.org

## Slide 37
Let’s go to some examples
Questions?
Acknowledgement
This lecture is supported by the project
of the EEA Grants with reg. num. EHP-CZ-ICP-3-012
of Brno University of Technology

## Slide 38: HPC – High Performance Computing
HPC introduction

## Slide 39: HPC – High Performance Computing

## Slide 40: HPC – High Performance Computing

## Slide 41: HPC – High Performance Computing
https://www.it4i.cz/en/research/research-flagships

## Slide 42: HPC – jobs submission

## Slide 43: HPC – High Performance Computing
#!/bin/bash
#PBS -N NAMEJOB
#PBS -l nodes=1:ppn=64:epyc7551
#PBS -l mem=120gb
#PBS -q default
##PBS -l walltime=2:00:00
cd $PBS_O_WORKDIR
module add vasp-6.3.0-openmpi-4.1.0
mpirun vasp_std >log.txt

## Slide 44: HPC – High Performance Computing

## Slide 45: HPC – High Performance Computing
https://www.it4i.cz/en/infrastructure/karolina

## Slide 46: Thank you!
www.eeagrants.org Facebook, Twitter, LinkedIn, Instagram YouTube: EEANorwayGrants Mail: info-fmo@efta.int